| Component - Plastics | E161723 |
| --- | --- |
| GE PLASTICS CHINA LTD |  |
| NANSHA E T D Z, 1 PLASTICS AVE WESTERN IND DISTRICT, PAN YU, GUANGZHOU GUANGDONG 511458 CN |  |
| 940A, 920A, 950A |  |
| Polycarbonate (PC), flame retardant, "Lexan", furnished as pellets |  |

|  | Min Thk | Flame |  |  | RTI | RTI | RTI |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Color | (mm) | Class | HWI | HAI | Elec | Imp | Str |
| ALL | 1.5 | V-2 | 3 | 1 | 130 | 120 | 125 |
|  | 2.3 | V-2 | 3 | - | 130 | 120 | 125 |
|  | 3.0 | V-0 | 2 | 3 | 130 | 120 | 130 |

| Comparative Tracking Index (CTI): | 2 | Dimensional Stability (%): | 0 |
| --- | --- | --- | --- |
| High-Voltage Arc Tracking Rate (HVTR): | 3 | High Volt, Low Current Arc Resis (D495): | 7 |
| Dielectric Strength (kV/mm): | 39 | Volume Resistivity (10xohm-cm): | 16 |

| NOTE - | Material designations may be followed by suffix numbers and or letters. |
| --- | --- |

UL94 small-scale test data does not pertain to building materials, furnishings and related contents. UL94 small-scale test data is intended solely for determining the flammability of plastic materials used in the components and parts of end-product devices and appliances, where the acceptability of the combination is determined by ULI.

| Report Date: 1994-12-16 Last Revised: 2003-10-24 | Underwriters Laboratories Inc® |  |
| --- | --- | --- |

IEC and ISO Test Methods

|  |  |  | Thickness |  |
| --- | --- | --- | --- | --- |
| Test Name | Test Method | Units | Tested (mm) | Value |
| IEC Flammability | IEC 60695-11-10 | Class (color) | 1.5 | V-2 (ALL) |
|  |  |  | 2.3 | V-2 (ALL) |
|  |  |  | 3.0 | V-0 (ALL) |
| Glow-Wire Flammability (GWFI) | IEC 60695-2-12 | C | - | - |
| Glow-Wire Ignition (GWIT) | IEC 60695-2-13 | C | - | - |
| IEC Comparative Tracking Index | IEC 60112 | Volts (Max) | - | - |
| IEC Ball Pressure | IEC 60695-10-2 | C | - | - |
| ISO Heat Deflection (1.80 MPa) | ISO 75-2 | C | - | - |
| ISO Tensile Strength | ISO 527-2 | MPa | - | - |
| ISO Flexural Strength | ISO 178 | MPa | - | - |
| ISO Tensile Impact | ISO 8256 | kJ/m2 | - | - |
| ISO Izod Impact | ISO 180 | kJ/m2 | - | - |
| ISO Charpy Impact | ISO 179-2 | kJ/m2 | - | - |

Underwriters Laboratories Inc®